MEDICAL GRADE PLASTIC STERILIZATION TECHNIQUES

| Material | Scientific name | Radiation | Autoclave (Steam) | EtO (Ethylene Oxide gas) |
| --- | --- | --- | --- | --- |
| PEEK | Polyether Ether Ketone (PEEK) | Excellent | Excellent | Excellent |
| TECASON P (Radel R) | ## Polyphenylsulfone (PPSU) | Excellent | Excellent | Excellent |
| TECANYL MT | Polyphenylene Oxyde (PPO) | Excellent | Excellent | Excellent |
| ULTEM 1000 | Polyether Imide (PEI) | Excellent | Good | Excellent |
| POLYSULFONE | Polysulfone (PS) | Excellent | Fair | Excellent |
| TECAPRO MT | Polypropylene (PP) | Poor | Excellent | Excellent |
| HYDEX 4101 PBT | PolyButylene Terephthalate (PBT) | Good | Poor | Excellent |
| HYDEX 4301 POLYCARBONATE | Polycarbonate (PC) | Good | Poor | Excellent |
| ACETAL |  | Poor | Fair | Excellent |